## Slide 1
Development of Mixed Organic Ionic Plastic Crystal Electrolytes for Energy Storage
Shanika Abeysooriya,1 Faezeh Makhlooghi Azad,1 Luke A. O’Dell,2 Jennifer M. Pringle,1
1Institute for Frontier Materials (IFM), Deakin University, Burwood Hwy, VIC 3125, Australia.
2Institute for Frontier Materials (IFM), Deakin University, Geelong, VIC 3220, Australia.
sabeysooriya@deakin.edu.au
Understanding the effect of combining OIPCs with two different cations has on the physicochemical and electrochemical properties and their potential use as solid-state electrolyte materials.
Research Aim
OIPCs (Organic Ionic Plastic Crystals)
Consist completely of cations and anions with a long range ordered crystalline lattice with short range disorder that occurs through rotational motions of molecules.1,2
Beneficial Features:
Good ionic conductivity
Negligible volatility
Goal:
Increase defects/ vacancies to tune physicochemical properties.
Introduction
Negligible flammability
Thermally stable
Varying mol % of [C(i3)mpyr][FSI] (5 – 90 mol %) were mixed with [C2epyr][FSI] to produce OIPC mixtures.
[C2epyr][FSI]
N,N-diethylpyrrolidinium bis(fluorosulfonyl)imide
[C(i3)mpyr][FSI]
N-isopropyl,N-methylpyrrolidinium
bis(fluorosulfonyl)imide
Synthetic Methodology
Phase behaviour of OIPC mixtures
With increasing [C(i3)mpyr][FSI] mol %,
Melting transitions move to higher temperatures. Melting peaks remain sharp.
Solid-solid phase transitions move to lower temperatures.
Presence of solid solutions.
Ionic conductivity properties of OIPC mixtures
When a small amount of slightly larger [C(i3)mpyr]+ is introduced, ionic conductivity increased compared to neat [C2epyr][FSI].
We assume this is due to increase in defects/ disorder in the OIPC mixture.
References
R. Yunis, T. W. Newbegin, A. F. Hollenkamp and J. M. Pringle, Mater. Chem. Front., 2018, 2, 1207–1214.
D. Al-Masri, R. Yunis, A. F. Hollenkamp, C. M. Doherty and J. M. Pringle, Phys. Chem. Chem. Phys., 2020, 22, 18102–18113.
10 mol % [C(i3)mpyr][FSI] added [C2epyr][FSI] mixture, showed high ionic conductivity compared to neat [C2epyr][FSI]. This hints to the increase in defects/ disorder when introducing a small of slightly larger cation ([C(i3)mpyr]+) to [C2epyr][FSI] OIPC system.
Li-salt added OIPC mixtures show promising results for potential use as solid-state electrolyte materials.
Conclusions
ifm.deakin.edu.au
Phase behaviour of Li-salt added OIPC mixtures
Li-salt added mixtures were quasi-solids at room temperature.
With 10 mol % LiFSI, melting transition decreases and broadens.
Neat [C2epyr][FSI]
Neat [C2epyr][FSI]
Neat [C(i3)mpyr][FSI]
10 mol % OIPC mixture
10 mol % OIPC mixture
Neat [C(i3)mpyr][FSI]
Results
Investigation of OIPC Mixtures as Potential Solid-state Electrolytes
Transport properties of Li-salt added OIPC mixtures
Li-salt added 10 mol % [C(i3)mpyr][FSI] binary mixture displayed slightly higher ionic conductivity than other mixtures.
This correlates with the ionic conductivity trends of the binary OIPC mixtures.
Morphology of Neat OIPCs and 10 mol% OIPC mixture