## Slide 1
Self-Assembly of CO2 Nonionic Surfactants in Ionic Liquids
Shurui Miao1, Michael Gradzielski2, Gregory Warr1
1. School of Chemistry and University of Sydney Nano Institute, The University of Sydney, NSW 2006, Australia
2. Institut für Chemie, Technische Universität Berlin, D-10623 Berlin, Germany
Greener Surfactant
Designer Solvent
Ionic liquids (ILs) are an emerging class of liquids purely composed of ions. Among many other favourable liquid properties, a display of diverse intermolecular interactions is common to many ILs. This enable them to be excellent mediums for self-assembly and they are known to support structures ranging from micelles to liquid crystals. As the solvent, ILs offer a platform with tuneable amphiphilicity and solvation behaviours,[2] making them promising solvent for the rational design of new functional soft matters.
QUOKKA @ ACNS
Model-Free Analysis
By assuming hard sphere interaction between micelles, we can estimate the solvation and softness.
CO2 wt% in Headgroup | Water[1] |  | EAN | 
0 | 0.01 | 1.72 | 1.70 | 3.18
4 | 0.37 | 1.64 | ---- | ----
10 | 0.50 | 1.63 | ---- | ----
12-14 | 0.52 | 1.58 | 1.54 | 2.33
27 | 0.55 | 1.51 | 1.25 | 2.04
CO2 wt% in Headgroup | Water[1] |  | EAN | 
0 | 0.01 | 1.72 | 1.70 | 3.18
4 | 0.37 | 1.64 | ---- | ----
10 | 0.50 | 1.63 | ---- | ----
12-14 | 0.52 | 1.58 | 1.54 | 2.33
27 | 0.55 | 1.51 | 1.25 | 2.04
Micelles are wetter and softer in EAN than water.
Although the trend is reversed, micelles are significantly wetter and softer in EAN than in water even at the highest CO2 content, confirming liquid crystal phases are missing.
Solvent-Headgroup interaction can be engineered through solvent composition and CO2:EO ratio!
References:
[1] V. J. Spiering, A. Ciapetti, M. T. Lima, D. W. Hayward, L. Noirez, M. S. Appavou, R. Schomacker, and M. Gradzielski, ChemSusChem 13, 601 (2020).
[2] R. Hayes, G. G. Warr, and R. Atkin, Chemical Reviews 115, 6357 (2015).
Water-loving Headgroup
Water-hating
tail